Submission ID: 100044507

Project #: LC465RD0003

Analysis: ICP OES, IC

prep={Hotplate:60 mL HCl, filter:False, for:K_ppm, Na_ppm}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-116611_1 | 0.2041 | 100 |
| 2-116611_2 | 0.1061 | 100 |

prep={Katanax:Ramping, filter:True, for:As_ppm, Ca_ppm}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-116611_1 | 0.2029 | 250 |
| 2-116611_2 | 0.2111 | 250 |

prep={hotplate:50 ml NaOH, filter:True, for:Cl}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-116611 | 4.0836 | 100 |

As_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 As |
| --- | --- | --- | --- | --- |
| 2-116611_1 | [+0.5 ppm, +1.0 ppm] [As] | 1.1x | n/a | <10.0 ppm |
| 2-116611_2 | [+0.5 ppm, +1.0 ppm] [As] | 1.1x | n/a | <10.0 ppm |

Ca_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Ca |
| --- | --- | --- | --- | --- |
| 2-116611_1 | [+0.5 ppm, +1.5 ppm] [Ca] | 1.7x | 1.057 | 2170.01 ppm |
| 2-116611_2 | [+0.5 ppm, +1.5 ppm] [Ca] | 1.7x | 1.118 | 2207.63 ppm |

Cl_ppm

| sample | Dilution | conc. [mg/L] | 000,0000 Cl | Blank=0.7808 mg/L |
| --- | --- | --- | --- | --- |
| 2-116611 | 1x | 1.5466 | 18.75 ppm |  |

K_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 K |
| --- | --- | --- | --- | --- |
| 2-116611_1 | [0.5 ppm, 1.0 ppm] [K] | 3.3x | 0.596 | 973.06 ppm |
| 2-116611_2 | [0.5 ppm, 1.0 ppm] [K] | 1.17x |  |  |

Na_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Na |
| --- | --- | --- | --- | --- |
| 2-116611_1 | [0.5 ppm, 1.0 ppm] [Na] | 3.3x | 0.653 | 1066.09 ppm |
| 2-116611_2 | [0.5 ppm, 1.0 ppm] [Na] | 1.17x |  |  |