Submission ID: 100044768

Project #: LC454RD0038

Analysis: Agilent OES

LOI

| sample | crucible (g) | crucible + sample (g) | crucible + sample + ∆ (g) | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-117247 |  |  |  |  |  |

prep={Katanax: Ramping, filter:True, for:Cu, Ni}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-117247_1 | 0.1999 | 250 |
| 2-117247_2 | 0.1932 | 250 |

prep={Hotplate: 60 mL HCl, filter:True, for:Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-117247_1 | 0.2040 | 100 |
| 2-117247_2 | 0.2060 | 100 |

pep={hotplate:50 ml NaOH, filter:True, for:NO3}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-117247_1 | 4.0213 | 100 |
| 2-117247_2 |  |  |

Cu

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu |
| --- | --- | --- | --- | --- |
| 2-117247_1 | [+0.5 ppm, +4.5 ppm] [Cu] | 20x | 3.453 | 8.64 |
| 2-117247_2 | [+0.5 ppm, +4.5 ppm] [Cu] | 20x | 3.331 | 8.62 |

NO3_ppm

| sample | Dilution | conc. [mg/L] | 000,0000 NO3 | Blank=0.3977 mg/L |
| --- | --- | --- | --- | --- |
| 2-117247_1 | 20x | 11.4716 | 5705.42 ppm |  |
| 2-117247_2 |  |  |  |  |

Na

| sample | analysis prep | Dilution | conc. [mg/L] | %Na |
| --- | --- | --- | --- | --- |
| 2-117247_1 | [0.5 ppm, 1.0 ppm] [Na] | 4.16x | 0.913 | 0.19 |
| 2-117247_2 | [0.5 ppm, 1.0 ppm] [Na] | 4.16x | 0.917 | 0.19 |

Ni

| sample | analysis prep | Dilution | conc. [mg/L] | %Ni |
| --- | --- | --- | --- | --- |
| 2-117247_1 | [+0.5 ppm, +4.0 ppm] [Ni] | 1.1x | 2.519 | 0.35 |
| 2-117247_2 | [+0.5 ppm, +4.0 ppm] [Ni] | 1.1x | 2.468 | 0.35 |

Cu lot: 26-30CUX exp: 2023-03-30

Na lot: 26-01NAY exp: 2023-04-30

Ni lot: 26-77NIT exp: 2023-07-30

Reference page 1-3 for formulas