Submission ID: 100045761

Project #: LP439RD0013

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 1000°F | after 900°C | LOI (%) | LOI (%) | correction ƒ | correction ƒ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |

prep={Katanax:Ramping, filter:False, for:Co, Cr, Ni}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| Batch #? | 0.2512 | 250 |
| Batch #? | 0.2500 | 250 |

Co

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Co | Avg(000,0000Co) |
| --- | --- | --- | --- | --- | --- |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Co] | 1.25x | 1.227 | 1526.34 ppm |  |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Co] | 1.25x | 1.316 | 1645.07 ppm | 1585.71 ppm |

Cr

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Cr | Avg(000,0000Cr) |
| --- | --- | --- | --- | --- | --- |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Cr] | 1.25x | 0.901 | 1120.93 ppm |  |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Cr] | 1.25x | 0.910 | 1137.91 ppm | 1129.42 ppm |

Ni

| sample | analysis prep | Dilution | conc. [mg/L] | %Ni | Avg(%Ni) |
| --- | --- | --- | --- | --- | --- |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Ni] | 6.6x | 2.358 | 1.56 |  |
| Batch #? | [+0.5 ppm, +3.5 ppm] [Ni] | 6.6x | 2.431 | 1.62 | 1.59 |

Co lot: 26-180COT exp: 2024-10-30

Cr lot: 4203E91 exp: 2024-03-01

Ni lot: 27-20NIT exp: 2024-10-30

Reference page for formulas

000,0000M+=conc.volumedilutionweight=M+ ppm

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]