Submission ID: 100046931

Project #: LC4990002

Analysis: ICP OES

| sample | weight (g) | volume (mL) | density [g/mL] |
| --- | --- | --- | --- |
| 2-123206 | 1.5968 | 1.0 | 1.5968 g/mL |

prep={HNO3,filter:False, for:Ce,Zr, Type:sol'n}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123206 | 0.3992 | 250 |

prep={HNO3,filter:False, for:Ti, Type:sol'n}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123206 | 3.1936 | 25 |

Ce

| sample | analysis prep | Dilution | conc. [mg/L] | %Ce |
| --- | --- | --- | --- | --- |
| 2-123206 | [0.5 ppm,2.5 ppm,5.0 ppm] [Ce] | 66.6x | 3.618 | 15.11 |

Ti_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Ti |
| --- | --- | --- | --- | --- |
| 2-123206 | [0.5 ppm,2.5 ppm,5.0 ppm] [Ti] | 12.5x | 1.030 | 8.06 ppm |

Zr

| sample | analysis prep | Dilution | conc. [mg/L] | %Zr |
| --- | --- | --- | --- | --- |
| 2-123206 | [0.5 ppm,2.5 ppm,5.0 ppm] [Zr] | 25x | 2.945 | 4.61 |

Ce lot: 27-167CEY exp: 2025-04-30

Ti lot: 27-189TIT exp: 2025-08-30

Zr lot: 27-151ZRY exp: 2025-10-30

Reference page for formulas

%M+=conc.volumedilutionweight*104

000,0000M+=conc.volumedilutionweight=ppm M+