Submission ID: 100047024

Project #: LP4130025

Analysis: ICP OES

LOI

| sample | crucible | crucible+sample | crucible + sample + ∆ (g) | LOI @760°C (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-123507 | 28.9528 | 30.9534 | 30.8128 | 7.03 | 0.9297 |

prep={Katanax:Ramping, filter:False, for:Ba,Ce, Ga,Si}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123507_1 | 0.2030 | 250 |
| 2-123507_2 | 0.2093 | 250 |

prep={Hotplate:60 mL HCl, filter:True, for:K}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123507_1 | 0.2069 | 200 |
| 2-123507_2 | 0.2097 | 200 |

prep={Hotplate:15 mL HCl, 5 mL HNO3 and 10 mL H2SO4, filter:True, for:Pt}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123507_1 | 0.5065 | 50 |
| 2-123507_2 | 0.5104 | 50 |

Ba

| sample | analysis prep | Dilution | conc. [mg/L] | %Ba | %Ba [dried] | Avg(%Ba) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [+0.5 ppm, +3.5 ppm] [Ba] | 50/15 | 2.084 | 0.86 | 0.92 |  |
| 2-123507_2 | [+0.5 ppm, +3.5 ppm] [Ba] | 50/15 | 2.149 | 0.86 | 0.92 | 0.92 |

Ce

| sample | analysis prep | Dilution | conc. [mg/L] | %Ce | %Ce [dried] | Avg(%Ce) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [+0.5 ppm, +3.5 ppm] [Ce] | 50/15 | 2.110 | 0.87 | 0.93 |  |
| 2-123507_2 | [+0.5 ppm, +3.5 ppm] [Ce] | 50/15 | 2.170 | 0.86 | 0.93 | 0.93 |

Ga

| sample | analysis prep | Dilution | conc. [mg/L] | %Ga | %Ga [dried] | Avg(%Ga) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [+0.5 ppm, +3.5 ppm] [Ga] | 50/6 | 2.184 | 2.24 | 2.41 |  |
| 2-123507_2 | [+0.5 ppm, +3.5 ppm] [Ga] | 50/6 | 2.237 | 2.23 | 2.40 | 2.41 |

K

| sample | analysis prep | Dilution | conc. [mg/L] | %K | %K [dried] | Avg(%K) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [0.5 ppm, 1.0 ppm] [K] | 25/7 | 1.038 | 0.36 | 0.39 |  |
| 2-123507_2 | [0.5 ppm, 1.0 ppm] [K] | 25/7 | 1.047 | 0.36 | 0.38 | 0.38 |

Pt_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Pt | 000,0000 Pt [dried] |
| --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [1.0 ppm, 1.5 ppm] [Pt] | 10/9 | 0.419 | 45.96 ppm | 49.43 ppm |
| 2-123507_2 | [1.0 ppm, 1.5 ppm] [Pt] | 10/9 | 0.472 | 45.61 ppm | 49.06 ppm |

SiO2

| sample | analysis prep | Dilution | conc. [mg/L] | %Si | %SiO2 | %SiO2 [dried] |
| --- | --- | --- | --- | --- | --- | --- |
| 2-123507_1 | [0.5 ppm, 2.5 ppm, 5.0 ppm] [Si] | 50/8 | 2.34 | 1.79 | 3.83 | 4.12 |
| 2-123507_2 | [0.5 ppm, 2.5 ppm, 5.0 ppm] [Si] | 50/8 | 2.560 | 1.91 | 4.09 | 4.40 |

Ba lot:

Ce lot: 27-167CEY exp: 2025-04-30

Ga lot:

K lot: 27-69KY exp: 2025-08-30

Pt lot: 27-99PTY exp: 2025-03-30

Si lot:

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=[B-A]-[C-A]B-A*100%

correction=[1-%LOI100]

%M+ dried=%M+correction

ppm M+[dried]=ppm M+correction

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104

%MO=[oxide factor]*%M+

%MO dried=%MOcorrection

ppm M+[dried]=ppm M+correction

%MO=MWMOMWM+*%M+