Submission ID:  100047141

Project #: LE4880001

Analysis: ICP OES

prep={method:Work Instruction, filter:True, for:Ag}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123917_1 | 0.5092 | 200 |
| 2-123917_2 | 0.5010 | 200 |

prep={Hotplate: 60 mL HCl, filter:True, for:Cs}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123917_1 | 1.2581 | 50 |
| 2-123917_2 | 1.2541 | 50 |

prep={method:Work Instruction, filter:True, for:Pd}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-123917_1 | 1.0028 | 200 |
| 2-123917_2 | 1.0088 | 200 |

Ag_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Ag | Avg() |
| --- | --- | --- | --- | --- | --- |
| 2-123917_1 | [+0.5 ppm, +2.5 ppm] [Ag] | 10/9 | 1.476 | 644.15 ppm |  |
| 2-123917_2 | [+0.5 ppm, +2.5 ppm] [Ag] | 10/9 | 1.468 | 651.14 ppm | 647.65 ppm |

Cs

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Cs | Avg() |
| --- | --- | --- | --- | --- | --- |
| 2-123917_1 | [50.0, 100.0, 200.0] [Cs] | 25/20 | 60.236 | 2992.41 ppm |  |
| 2-123917_2 | [50.0, 100.0, 200.0] [Cs] | 25/20 | 61.207 | 3050.34 ppm | 3021.38 ppm |

Pd_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Pd | Avg() |
| --- | --- | --- | --- | --- | --- |
| 2-123917_1 | [+0.5 ppm, +3.5 ppm] [Pd] | 10/5 | 1.353 | 539.69 ppm |  |
| 2-123917_2 | [+0.5 ppm, +3.5 ppm] [Pd] | 10/5 | 1.363 | 540.44 ppm | 540.07 ppm |

Ag lot: 26-169AGY exp: 2025-02-28

Cs lot: 27-42CSY exp: 2025-03-30

Pd lot: 27-164PDY exp: 2026-02-28

Reference page for formulas

000,0000M+=conc.volumedilutionweight=ppm M+