Submission ID: MegaMax 800

Project #: Analytical

Analysis: Agilent OES

prep={Microwave, filter:False, for:Al, Cu, Zn}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.1185 | 200 |
| sample_2 | 0.1034 | 200 |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | Avg(%Al) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Al] | 100/10 | 2.198 | 3.71 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Al] | 100/10 | 1.910 | 3.69 | 3.70 |

Cu

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu | Avg(%Cu) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/1 | 1.985 | 33.50 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/1 | 1.695 | 32.79 | 33.15 |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | Avg(%Zn) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/2 | 1.819 | 15.35 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/2 | 1.584 | 15.32 | 15.34 |

| Element | Metal [%] | Oxide [%] |
| --- | --- | --- |
| Al | 3.70 | 6.99 |
| Cu | 33.15 | 41.50 |
| Zn | 15.34 | 19.10 |
| Total |  | 67.59 |

Al lot: 27-171ALT exp: 2025-07-30

Cu lot: 27-156CUY exp: 2026-02-28

Zn lot: 27-149ZNY exp: 2025-10-30

Reference page for formulas

%M+=conc.volumedilutionweight*104