Submission ID: ShiftMax 150

Project #: Analytical

Analysis: Agilent OES

prep={Microwave, filter:False, for:Al, Cu, Zn}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.1007 | 200 |
| sample_2 | 0.1087 | 200 |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | Avg(%Al) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Al] | 50/2 | 2.026 | 10.06 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Al] | 50/2 | 2.118 | 9.74 | 9.90 |

Cu

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu | Avg(%Cu) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Cu] | 50/10 | 2.131 | 2.12 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Cu] | 50/10 | 2.248 | 2.07 | 2.10 |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | Avg(%Zn) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.5 | 1.754 | 34.84 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.5 | 1.846 | 33.97 | 34.41 |

| Element | Metal [%] | Oxide [%] |
| --- | --- | --- |
| Al | 9.90 | 18.70 |
| Cu | 2.10 | 2.63 |
| Zn | 34.41 | 42.84 |
| Total |  | 64.17 |

Al lot: 27-171ALT exp: 2025-07-30

Cu lot: 27-156CUY exp: 2026-02-28

Zn lot: 27-149ZNY exp: 2025-10-30

Reference page for formulas

%M+=conc.volumedilutionweight*104