Submission ID: ShiftMax 150

Project #: Analytical

Analysis: Agilent OES

prep={Microwave, filter:False, for:Al, Cu, Zn}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.1031 | 200 |
| sample_2 | 0.1065 | 200 |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | Avg(%Al) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Al] | 100/3 | 2.325 | 15.03 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Al] | 100/3 | 2.175 | 13.62 | 14.32 |

Cu

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu | Avg(%Cu) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Cu] | 50/5 | 1.816 | 3.52 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Cu] | 50/5 | 1.817 | 3.41 | 3.47 |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | Avg(%Zn) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.5 | 2.553 | 49.52 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.5 | 2.654 | 49.84 | 49.68 |

| Element | Metal [%] | Oxide [%] |
| --- | --- | --- |
| Al | 14.32 | 27.05 |
| Cu | 3.47 | 4.34 |
| Zn | 49.68 | 61.85 |
| Total |  | 93.24 |

Al lot: 27-171ALT exp: 2025-07-30

Cu lot: 27-156CUY exp: 2026-02-28

Zn lot: 27-149ZNY exp: 2025-10-30

Reference page for formulas

%M+=conc.volumedilutionweight*104