Submission ID: 100047371

Project #: LC4990007

Analysis: ICP

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-124637 | 25.6955 | 27.6959 | 27.6724 | 1.17 | 0.9883 |
| 2-124638 | 25.5990 | 27.6038 | 27.5582 | 2.27 | 0.9773 |
| 2-124639 | 25.6557 | 27.6603 | 27.6353 | 1.25 | 0.9875 |

prep={method:Work Instruction, filter:True, for:Pd}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-124639_1 | 1.0062 | 200 |
| 2-124639_2 | 1.0029 | 200 |

prep={Hotplate:15 mL HCl, 5 mL HNO3 and 10 mL H2SO4, filter:True, for:Pt}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-124637_1 | 0.5045 | 50 |
| 2-124637_2 | 0.5048 | 50 |
| 2-124638_1 | 0.5061 | 50 |
| 2-124638_2 | 0.5077 | 50 |

prep={High Ti method, filter:False, for:W, Zr}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-124637_1 | 0.3059 | 250 |
| 2-124637_2 | 0.3077 | 250 |
| 2-124638_1 | 0.3031 | 250 |
| 2-124638_2 | 0.3101 | 250 |
| 2-124639_1 | 0.3055 | 250 |
| 2-124639_2 | 0.3028 | 250 |

Pd

| sample | analysis prep | Dilution | conc. [mg/L] | %Pd | %Pd [dried] | Avg(%Pd) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-124639_1 | [+0.5 ppm, +3.5 ppm] [Pd] | 100/3 | 1.546 | 1.02 | 1.04 |  |
| 2-124639_2 | [+0.5 ppm, +3.5 ppm] [Pd] | 100/3 | 1.586 | 1.05 | 1.07 | 1.05 |

Pt

| sample | analysis prep | Dilution | conc. [mg/L] | %Pt | %Pt [dried] | Avg(%Pt) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-124637_1 | [+0.5 ppm, +3.5 ppm] [Pt] | 50/2 | 2.208 | 0.55 | 0.55 |  |
| 2-124637_2 | [+0.5 ppm, +3.5 ppm] [Pt] | 50/2 | 2.265 | 0.56 | 0.57 | 0.56 |
| 2-124638_1 | [+0.5 ppm, +3.5 ppm] [Pt] | 50/1 | 2.027 | 1.00 | 1.02 |  |
| 2-124638_2 | [+0.5 ppm, +3.5 ppm] [Pt] | 50/1 | 1.816 | 0.89 | 0.91 | 0.97 |

W

| sample | analysis prep | Dilution | conc. [mg/L] | %W | %W [dried] | Avg(%W) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-124637_1 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 | 3.497 | 14.29 | 14.46 | 14.46 |
| 2-124637_2 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 |  |  |  |  |
| 2-124638_1 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 | 3.385 | 13.96 | 14.28 | 14.28 |
| 2-124638_2 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 |  |  |  |  |
| 2-124639_1 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 | 3.460 | 14.16 | 14.34 | 14.34 |
| 2-124639_2 | [+0.5 ppm, +3.5 ppm] [W] | 100/2 |  |  |  |  |

Zr

| sample | analysis prep | Dilution | conc. [mg/L] | %Zr | %Zr [dried] | Avg(%Zr) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-124637_1 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 | 1.910 | 62.44 | 63.18 |  |
| 2-124637_2 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 |  |  |  |  |
| 2-124638_1 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 | 1.803 | 59.49 | 60.87 |  |
| 2-124638_2 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 |  |  |  |  |
| 2-124639_1 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 | 1.802 | 58.99 | 59.73 |  |
| 2-124639_2 | [+0.5 ppm, +3.5 ppm] [Zr] | 100/0.25 |  |  |  |  |

Manufacturer: Assurance, Pd lot: 27-164PDY exp: 2026-02-28

Manufacturer: Assurance, Pt lot: 28-2PTY exp: 2026-03-30

Manufacturer: Ricca, W lot: 4505R15 exp: 2026-11-30

Manufacturer: Assurance, Zr lot: 27-151ZRY exp: 2025-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]