Submission ID: Au, Ti

Project #: Analytical

Analysis: Agilent OES

pprep={Microwave, filter:True, for:Au, Ti}}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.1057 | 200 |
| sample_2 | 0.1036 | 200 |

Au

| sample | analysis prep | Dilution | conc. [mg/L] | %Au | Avg(%Au) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Au] | 25/7 | 2.154 | 1.46 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Au] | 25/7 | 2.181 | 1.50 | 1.48 |

Ti from microwave digestion

| sample | analysis prep | Dilution | conc. [mg/L] | %Ti | Avg(%Ti) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Ti] | 25/15 | 2.457 | 0.77 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Ti] | 25/15 | 2.518 | 0.81 | 0.79 |

Ti from HF digestion

| sample | analysis prep | Dilution | conc. [mg/L] | %Ti | Avg(%Ti) |
| --- | --- | --- | --- | --- | --- |
| 2-124589_1 | [+0.5 ppm, +3.5 ppm] [Ti] | 100/4 | 2.246 | 5.48 |  |
| 2-124589_2 | [+0.5 ppm, +3.5 ppm] [Ti] | 100/4 | 2.276 | 5.55 | 5.52 |

Au lot: 27-144AUY exp: 2026-01-30

Ti lot: 27-189TIT exp: 2025-08-30

Reference page for formulas

%M+=conc.volumedilutionweight*104