Submission ID: FTMax

Project #: Analytical

Analysis: Agilent OES

prep={Microwave, filter:True, for:Co, Pt}}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.2250 | 100 |
| sample_2 | 0.2187 | 100 |

Co

| sample | analysis prep | Dilution | conc. [mg/L] | %Co | Avg(%Co) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Co] | 100/0.385 | 1.792 | 21.46 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Co] | 100/0.385 | 1.859 | 22.08 | 21.77 |

Pt_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Pt | Avg(000,0000 Pt) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +1.5 ppm] [Pt] | 10/9 | 0.695 | 343.21 ppm |  |
| sample_2 | [+0.5 ppm, +1.5 ppm] [Pt] | 10/9 | 0.677 | 353.10 ppm | 348.16 ppm |

Co lot: 26-34COT exp: 2023-11-30

Pt lot: 26-03PTY exp: 2023-05-30

Reference page 1-3 for formulas

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104