Submission ID: Ga, La

Project #: Analytical

Analysis: Agilent OES

prep={Microwave, filter:True, for:Ga, La}}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| sample_1 | 0.1034 | 200 |
| sample_2 | 0.1096 | 200 |

Ga

| sample | analysis prep | Dilution | conc. [mg/L] | %Ga | Avg(%Ga) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [Ga] | 50/10 | 1.935 | 1.87 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [Ga] | 50/10 | 2.081 | 1.90 | 1.89 |

La

| sample | analysis prep | Dilution | conc. [mg/L] | %La | Avg(%La) |
| --- | --- | --- | --- | --- | --- |
| sample_1 | [+0.5 ppm, +3.5 ppm] [La] | 25/8 | 1.872 | 1.13 |  |
| sample_2 | [+0.5 ppm, +3.5 ppm] [La] | 25/8 | 1.946 | 1.11 | 1.12 |

La lot: 27-169LAY exp: 2026-02-28

Reference page for formulas

%M+=conc.volumedilutionweight*104