Submission ID: 100047771

Project #: LC454RD0034

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-125827 | 26.8162 | 28.8163 | 28.6105 | 10.29 | 0.8971 |
| 2-125828 | 26.3199 | 28.3205 | 28.0831 | 11.87 | 0.8813 |

prep={Katanax: Ramping, filter:False, for:Al,Fe, Zn}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-125827_1 | 0.2023 | 250 |
| 2-125827_2 | 0.2047 | 250 |
| 2-125828_1 | 0.2047 | 250 |
| 2-125828_2 | 0.2061 | 250 |

prep={Hotplate:60 mL 1:1 HCl, filter:False, for:Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-125827_1 | 0.2062 | 200 |
| 2-125827_2 | 0.2039 | 200 |
| 2-125828_1 | 0.2083 | 200 |
| 2-125828_2 | 0.2051 | 200 |

pep={hotplate:50 ml NaOH, filter:True, for:NO3}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-125827 | 1.0041 | 100 |
| 2-125828 | 1.0080 | 100 |

prep={Microwave:9 mL HCl, 3 mL HNO3, 3 mL H2SO4, filter:False, for:Al, Fe, Na, Zn}}

| sample | weight (g) | volume (mL) | Time (min) | Power (W) | T1 (°C) | T2 (°C) | P (bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-125827_1 | 0.1083 | 250 | 60 | 1500 | 260 | 65 | 110 |
| 2-125827_2 | 0.1053 | 250 |  |  |  |  |  |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | %Al2O3 | [dried] | Avg(%Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-125827_1 | [+0.5 ppm, +3.5 ppm] [Al] | 100/5 | 1.963 | 4.85 | 9.16 | 10.21 |  |
| 2-125827_2 | [+0.5 ppm, +3.5 ppm] [Al] | 100/5 | 1.952 | 4.77 | 9.01 | 10.04 | 10.13 |
| 2-125828_1 | [+0.5 ppm, +3.5 ppm] [Al] | 100/5 | 1.988 | 4.86 | 9.17 | 10.40 |  |
| 2-125828_2 | [+0.5 ppm, +3.5 ppm] [Al] | 100/5 | 2.008 | 4.87 | 9.20 | 10.44 | 10.42 |
| 2-125828_1 | [+0.5 ppm, +3.5 ppm] [Al] | 50/5 | 2.079 | 4.80 | 9.07 | 10.11 |  |
| 2-125828_2 | [+0.5 ppm, +3.5 ppm] [Al] | 50/5 | 1.908 | 4.53 | 8.56 | 9.54 |  |

Fe

| sample | analysis prep | Dilution | conc. [mg/L] | %Fe | %Fe2O3 | [dried] | Avg(%Fe2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-125827_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/0.662 | 2.052 | 38.31 | 54.78 | 61.06 |  |
| 2-125827_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/0.662 | 1.977 | 36.47 | 52.16 | 58.14 |  |
| 2-125828_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/0.75 | 2.073 | 33.76 | 48.27 | 54.77 |  |
| 2-125828_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/0.75 | 1.982 | 32.06 | 45.84 | 52.01 |  |
| 2-125827_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 | 1.675 | 38.67 | 55.29 | 61.63 |  |
| 2-125827_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 | 1.612 | 38.27 | 54.73 | 61.01 | 61.32 |

Na

| sample | analysis prep | Dilution | conc. [mg/L] | %Na | %Na2O | [dried] | Avg(%Na2O) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-125827_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/1 | 1.037 | 5.03 | 6.78 | 7.56 |  |
| 2-125827_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/1 | 1.016 | 4.98 | 6.72 | 7.49 | 7.53 |
| 2-125828_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/1 | 1.083 | 5.20 | 7.01 | 7.95 |  |
| 2-125828_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/1 | 1.050 | 5.12 | 6.90 | 7.83 | 7.89 |
| 2-125827_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/2 | 0.869 | 5.02 | 6.76 | 7.54 |  |
| 2-125827_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/2 | 0.842 | 5.00 | 6.74 | 7.51 | 7.53 |

NO3_ppm

| sample | Dilution | conc. [mg/L] | 000,0000 NO3 | 000,0000 NO3 [dried] |
| --- | --- | --- | --- | --- |
| 2-125827 | 25/8 | 9.3644 | 2914.43 ppm | 3248.72 ppm |
| 2-125828 | 100/100 | 11.5112 | 1141.98 ppm | 1295.79 ppm |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | %ZnO | [dried] | Avg(%ZnO) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-125827_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.625 | 1.833 | 18.12 | 22.56 | 25.15 |  |
| 2-125827_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.625 | 1.744 | 17.04 | 21.21 | 23.64 | 24.40 |
| 2-125828_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.625 | 1.809 | 17.67 | 22.00 | 24.96 |  |
| 2-125828_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 50/0.625 | 1.817 | 17.63 | 21.95 | 24.91 | 24.94 |
| 2-125827_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/3 | 2.342 | 18.02 | 22.44 | 25.01 |  |
| 2-125827_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/3 | 2.279 | 18.04 | 22.45 | 25.02 | 25.02 |

Manufacturer: Assurance, Al lot: 27-171ALT exp: 2026-07-30

Manufacturer: Assurance, Fe lot: 28-75FEY exp: 2026-07-30

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Ricca, NO3 lot: 4410M47 exp: 2026-04-30

Manufacturer: Assurance, Zn lot: 27-149ZNY exp: 2025-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]