Submission ID: 100047903

Project #: LC4990010

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-126125 | 27.5857 | 29.5879 | 29.5580 | 1.49 | 0.9851 |

prep={Katanax:Ramping, filter:False, for:Cu, Fe}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126125_1 | 0.2083 | 250 |
| 2-126125_2 | 0.2045 | 250 |

prep={Hotplate:60 mL HCl, filter:False, for:K}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126125_1 | 0.2055 | 100 |
| 2-126125_2 | 0.2087 | 100 |

CuO

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu | %CuO | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126125_1 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/0.5 | 2.171 | 52.11 | 65.24 | 66.23 |  |
| 2-126125_2 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/0.5 | 2.113 | 51.66 | 64.68 | 65.66 | 65.95 |

Fe2O3

| sample | analysis prep | Dilution | conc. [mg/L] | %Fe | %Fe2O3 | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126125_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 | 1.916 | 23.00 | 32.88 | 33.38 |  |
| 2-126125_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 | 1.871 | 22.87 | 32.71 | 33.20 | 33.29 |

K2O

| sample | analysis prep | Dilution | conc. [mg/L] | %K | %K2O | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126125_1 | [0.5 ppm, 1.0 ppm] [K] | 100/5 | 0.853 | 0.83 | 1.00 | 1.01 |  |
| 2-126125_2 | [0.5 ppm, 1.0 ppm] [K] | 100/5 | 0.885 | 0.85 | 1.02 | 1.03 | 1.02 |

Manufacturer: Assurance, Cu lot: 27-156CUY exp: 2026-02-28

Manufacturer: Assurance, Fe lot: 28-75FEY exp: 2026-07-30

Manufacturer: Assurance, K lot: 28-6KY exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]