Submission ID: 100047938

Project #: LC454RD0030

Analysis: Agilent OES, IC

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-126191 | 28.1698 | 30.1760 | 30.1517 | 1.21 | 0.9879 |
| 2-126192 | 26.1968 | 28.1948 | 28.1704 | 1.22 | 0.9878 |

prep={hotplate:50 ml NaOH, filter:True, for:Cl}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126191 | 1.0096 | 100 |
| 2-126192 | 1.0058 | 100 |

prep={Katanax: Ramping, filter:False, for:Fe, Ni}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126191_1 | 0.3023 | 250 |
| 2-126191_2 | 0.3038 | 250 |
| 2-126192_1 | 0.3036 | 250 |
| 2-126192_2 | 0.3064 | 250 |

prep={Hotplate:60 mL 1:1 HCl, filter:True, for:Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126191_1 | 0.5054 | 50 |
| 2-126191_2 | 0.5072 | 50 |
| 2-126192_1 | 0.5021 | 50 |
| 2-126192_2 | 0.5042 | 50 |

prep={method:Work Instruction, filter:False, for:Ru}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126191_1 | 0.3053 | 250 |
| 2-126191_2 | 0.3089 | 250 |
| 2-126192_1 | 0.3084 | 250 |
| 2-126192_2 | 0.3047 | 250 |

Cl

| sample | Dilution | conc. [mg/L] | %Cl | %Cl [dried] |
| --- | --- | --- | --- | --- |
| 2-126191 | 25/3 | 10.6400 | 0.88 | 0.89 |
| 2-126192 | 25/3 | 10.5266 | 0.87 | 0.88 |

Fe_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Fe | [dried] | Avg(000,0000Fe) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126191_1 | [+0.5 ppm, +1.0 ppm] [Fe] | 10/9 | 0.191 | 175.51 ppm | 177.66 |  |
| 2-126191_2 | [+0.5 ppm, +1.0 ppm] [Fe] | 10/9 | 0.176 | 160.92 ppm | 162.90 | 170.28 ppm |
| 2-126192_1 | [+0.5 ppm, +1.0 ppm] [Fe] | 10/9 | 0.187 | 171.10 ppm | 173.21 |  |
| 2-126192_2 | [+0.5 ppm, +1.0 ppm] [Fe] | 10/9 | 0.179 | 162.28 ppm | 164.28 | 168.75 ppm |

Na_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Na | [dried] | Avg(000,0000Na) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126191_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/50 | 0.564 | 55.80 ppm | 56.48 |  |
| 2-126191_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/50 | 0.499 | 49.19 ppm | 49.79 | 53.14 ppm |
| 2-126192_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/50 | 0.434 | 43.22 ppm | 43.75 |  |
| 2-126192_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/50 | 0.427 | 42.34 ppm | 42.87 | 43.31 ppm |

Ni

| sample | analysis prep | Dilution | conc. [mg/L] | %Ni | [dried] | Avg(%Ni) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126191_1 | [+0.5 ppm, +3.5 ppm] [Ni] | 100/1.6 | 2.029 | 10.07 | 10.20 |  |
| 2-126191_2 | [+0.5 ppm, +3.5 ppm] [Ni] | 100/1.6 | 2.041 | 10.08 | 10.20 | 10.20 |
| 2-126192_1 | [+0.5 ppm, +3.5 ppm] [Ni] | 100/1.6 | 2.008 | 9.92 | 10.05 |  |
| 2-126192_2 | [+0.5 ppm, +3.5 ppm] [Ni] | 100/1.6 | 2.027 | 9.93 | 10.05 | 10.05 |

Ru

| sample | analysis prep | Dilution | conc. [mg/L] | %Ru | [dried] | Avg(%Ru) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126191_1 | [+0.5 ppm, +3.5 ppm] [Ru] | 25/6 | 2.043 | 0.69 | 0.70 |  |
| 2-126191_2 | [+0.5 ppm, +3.5 ppm] [Ru] | 25/6 | 2.049 | 0.69 | 0.70 | 0.70 |
| 2-126192_1 | [+0.5 ppm, +3.5 ppm] [Ru] | 25/6 | 2.037 | 0.69 | 0.70 |  |
| 2-126192_2 | [+0.5 ppm, +3.5 ppm] [Ru] | 25/6 | 2.090 | 0.71 | 0.72 | 0.71 |

Manufacturer: Ricca, Cl lot: 2502C26 exp: 2027-01-31

Manufacturer: Assurance, Fe lot: 28-75FEY exp: 2026-07-30

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Ni lot: 27-186NIT exp: 2026-02-28 [EXPIRED]

Manufacturer: Assurance, Ru lot: 28-56RUY exp: 2026-05-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Reference page for formulas

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104