Submission ID: 100048032

Project #: LC403TS-25-3773

Sample prep: None.

Analysis: Agilent OES

prep={Katanax: Ramping, filter:False, for:Al,Ca,La, Si}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126512_1 | 0.3038 | 250 |
| 2-126512_2 | 0.3049 | 250 |

prep={Hotplate:60 mL 1:1 HCl, filter:True, for:K,Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126512_1 | 0.3040 | 50 |
| 2-126512_2 | 0.3059 | 50 |

Al_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Al | Avg(000,0000Al) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [+0.5 ppm, +1.5 ppm] [Al] | 10/9 | 0.949 | 867.71 ppm |  |
| 2-126512_2 | [+0.5 ppm, +1.5 ppm] [Al] | 10/9 | 0.903 | 822.67 ppm | 845.19 ppm |

Ca_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Ca | Avg(000,0000Ca) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [+0.5 ppm, +3.5 ppm] [Ca] | 10/9 | 2.221 | 2030.76 ppm |  |
| 2-126512_2 | [+0.5 ppm, +3.5 ppm] [Ca] | 10/9 | 2.171 | 1977.88 ppm | 2004.32 ppm |

K_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000K | Avg(000,0000K) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [0.5 ppm, 1.0 ppm] [K] | 50/2 | 0.830 | 3412.83 ppm |  |
| 2-126512_2 | [0.5 ppm, 1.0 ppm] [K] | 50/2 | 0.832 | 3399.80 ppm | 3406.32 ppm |

La_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000La | Avg(000,0000La) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [+0.5 ppm, +1.0 ppm] [La] | 10/9 | N/A | <10.0 ppm |  |
| 2-126512_2 | [+0.5 ppm, +1.0 ppm] [La] | 10/9 | N/A | <10.0 ppm | <10.0 ppm |

Na_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000Na | Avg(000,0000Na) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [0.5 ppm, 1.0 ppm] [Na] | 25/10 | 0.892 | 366.78 ppm |  |
| 2-126512_2 | [0.5 ppm, 1.0 ppm] [Na] | 25/10 | 0.888 | 362.86 ppm | 364.82 ppm |

Si_ppm

| sample | analysis prep | Dilution | conc. [mg/L] | 000,0000 Si | Avg(Si_ppm) |
| --- | --- | --- | --- | --- | --- |
| 2-126512_1 | [0.5, 2.5, 5.0 ppm] [Si] | 25/10 | 2.608 | 5365.37 ppm |  |
| 2-126512_2 | [0.5, 2.5, 5.0 ppm] [Si] | 25/10 | 2.591 | 5311.17 ppm | 5338.27 ppm |

Manufacturer: Assurance, Al lot: 27-171ALT exp: 2026-07-30

Manufacturer: Assurance, Ca lot: 28-35CAY exp: 2026-10-30

Manufacturer: Assurance, K lot: 28-6KY exp: 2026-08-30

Manufacturer: Assurance, La lot: 27-169LAY exp: 2026-02-28

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Si lot: 28-87SIX exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Reference page for formulas

000,0000M+=conc.volumedilutionweight=ppm M+