Submission ID: 100047966

Project #: LP4130022

Analysis: Agilent OES and Metrohm titrator

Cr(VI)

| sample | weight (g) | volume (mL) | %Cr(VI) | Avg(%Cr6+) | FAS=0.0842 N |
| --- | --- | --- | --- | --- | --- |
| 2-126266_1 | 4.5039 | 0.87704 | 0.028 |  |  |
| 2-126266_2 | 4.5042 | 0.79607 | 0.026 | 0.027 |  |

Cr2O3

| sample | weight (g) | volume (mL) | %Cr2O3 | Avg(%Cr2O3) | FAS |
| --- | --- | --- | --- | --- | --- |
| 2-126266_1 | 0.10 |  | Catofin 310-Cr, Na, Zr_RD3 |  |  |
| 2-126266_2 | 0.10 |  | Catofin 310-Cr, Na, Zr_RD3 |  |  |

prep={20 ml H2SO4, filter:False, for:Na,Zr}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126266_1 | 0.3048 | 200 |
| 2-126266_2 | 0.3045 | 200 |

prep={60 ml HCl, filter:True, for:Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126266_1 | 0.2056 | 200 |
| 2-126266_2 | 0.2032 | 200 |

Na2O

| sample | analysis prep | Dilution | conc. [mg/L] | %Na | %Na2O | Avg(%Na2O) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126266_1 | [0.5 ppm, 1.0 ppm] [Na] | 25/5 | 0.694 | 0.34 | 0.46 |  |
| 2-126266_2 | [0.5 ppm, 1.0 ppm] [Na] | 25/5 | 0.677 | 0.33 | 0.45 | 0.46 |

Zr

| sample | analysis prep | Dilution | conc. [mg/L] | %Zr | %ZrO2 | Avg(%ZrO2) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-126266_1 | [+0.5 ppm, +3.5 ppm] [Zr] | 25/10 | Catofin 310-Cr, Na, Zr_RD3 |  |  |  |
| 2-126266_2 | [+0.5 ppm, +3.5 ppm] [Zr] | 25/10 | Catofin 310-Cr, Na, Zr_RD3 |  |  |  |

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Manufacturer: Assurance, Zr lot: 28-64ZRY exp: 2026-10-30

Reference page for formulas

%CrVI=1.733mL FAS[N FAS][weight]

%Cr2O3=1.462*[%Cr(VI)]

%M+=conc.volumedilutionweight*104

%MO=MWMOMWM+*%M+