Submission ID: 100048023

Project #: LC4990010

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-126485 | 28.1186 | 30.1293 | 30.1071 | 1.10 | 0.9890 |

prep={Katanax:Ramping, filter:False, for:Al,Cu, Fe}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126485_1 | 0.2015 | 250 |
| 2-126485_2 | 0.2067 | 250 |

prep={Hotplate:60 mL HCl, filter:True, for:K}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126485_1 | 0.2022 | 200 |
| 2-126485_2 | 0.2054 | 200 |

prep={Hotplate:HF, filter:False, for:Si}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-126485_1 | 0.1065 | 250 |
| 2-126485_2 | 0.1063 | 250 |

Al2O3

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | %Al2O3 | [dried] | Avg(%Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126485_1 | [+0.5 ppm, +3.5 ppm] [Al] | 25/4 | 1.882 | 1.46 | 2.76 | 2.79 |  |
| 2-126485_2 | [+0.5 ppm, +3.5 ppm] [Al] | 25/4 | 1.843 | 1.40 | 2.65 | 2.68 | 2.73 |

CuO

| sample | analysis prep | Dilution | conc. [mg/L] | %Cu | %CuO | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126485_1 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/0.6 | 1.995 | 41.25 | 51.65 | 52.22 |  |
| 2-126485_2 | [+0.5 ppm, +3.5 ppm] [Cu] | 100/0.6 | 2.049 | 41.30 | 51.71 | 52.29 | 52.26 |

Fe2O3

| sample | analysis prep | Dilution | conc. [mg/L] | %Fe | %Fe2O3 | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126485_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 50/0.7 | 2.083 | 18.46 | 26.40 | 26.69 |  |
| 2-126485_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 50/0.7 | 2.065 | 17.84 | 25.51 | 25.79 | 26.24 |

K2O

| sample | analysis prep | Dilution | conc. [mg/L] | %K | %K2O | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126485_1 | [0.5 ppm, 1.0 ppm] [K] | 50/4 | 0.625 | 0.77 | 0.93 | 0.94 |  |
| 2-126485_2 | [0.5 ppm, 1.0 ppm] [K] | 50/4 | 0.646 | 0.79 | 0.95 | 0.96 | 0.95 |

SiO2

| sample | analysis prep | Dilution | conc. [mg/L] | %Si | %SiO2 | [dried] | Avg() |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-126485_1 | [0.5 ppm, 2.5 ppm, 5.0 ppm] [Si] | 100/8 | 3.315 | 9.73 | 20.81 | 21.04 | 21.04 |
| 2-126485_2 | [0.5 ppm, 2.5 ppm, 5.0 ppm] [Si] | 100/8 | 4.035 |  |  |  |  |

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]