Submission ID: 100048288

Project #: LC454RD0034

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-127234 | 23.3441 | 25.3448 | 25.1998 | 7.25 | 0.9275 |

prep={Katanax: Ramping, filter:True, for:Al,Fe, Zn}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127234_1 | 0.2077 | 250 |
| 2-127234_2 | 0.2066 | 250 |

prep={Hotplate:60 mL 1:1 HCl, filter:True, for:Na}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127234_1 | 0.1011 | 250 |
| 2-127234_2 | 0.1083 | 250 |

prep={Microwave:9 mL HCl, 3 mL HNO3, 3 mL H2SO4, filter:True, for:Al, Fe, Na, Zn}}

| sample | weight (g) | volume (mL) | Time (min) | Power (W) | T1 (°C) | T2 (°C) | P (bar) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127234_1 | 0.10 | 250 | 60 | 1500 | 260 | 65 | 110 |
| 2-127234_2 | 0.10 | 250 |  |  |  |  |  |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | %Al2O3 | [dried] | Avg(%Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127234_1 | [+1.0 ppm, +3.0 ppm] [Al] | 50/3 | 1.682 | 3.37 | 6.37 | 6.87 |  |
| 2-127234_2 | [+1.0 ppm, +3.0 ppm] [Al] | 50/3 | 1.694 | 3.42 | 6.45 | 6.95 | 6.91 |
| 2-127234_1 | [+1.0 ppm, +3.0 ppm] [Al] | 50/5 |  |  |  |  |  |
| 2-127234_2 | [+1.0 ppm, +3.0 ppm] [Al] | 50/5 |  |  |  |  |  |

Fe

| sample | analysis prep | Dilution | conc. [mg/L] | %Fe | %Fe2O3 | [dried] | Avg(%Fe2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127234_1 | [+1.0 ppm, +3.0 ppm] [Fe] | 100/1 | 1.823 | 21.94 | 31.38 | 33.83 |  |
| 2-127234_2 | [+1.0 ppm, +3.0 ppm] [Fe] | 100/1 | 1.818 | 22.00 | 31.46 | 33.92 | 33.87 |
| 2-127234_1 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 |  |  |  |  |  |
| 2-127234_2 | [+0.5 ppm, +3.5 ppm] [Fe] | 100/1 |  |  |  |  |  |

Na

| sample | analysis prep | Dilution | conc. [mg/L] | %Na | %Na2O | [dried] | Avg(%Na2O) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127234_1 | [0.5 ppm, 1.0 ppm] [Na] | 200/3 | 0.961 | 15.84 | 21.36 | 23.03 |  |
| 2-127234_2 | [0.5 ppm, 1.0 ppm] [Na] | 200/3 | 1.032 | 15.88 | 21.41 | 23.08 | 23.06 |
| 2-127234_1 | [0.5 ppm, 1.0 ppm] [Na] | 50/2 |  |  |  |  |  |
| 2-127234_2 | [0.5 ppm, 1.0 ppm] [Na] | 50/2 |  |  |  |  |  |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | %ZnO | [dried] | Avg(%ZnO) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127234_1 | [+1.0 ppm, +3.0 ppm] [Zn] | 50/1 | 2.054 | 12.36 | 15.39 | 16.59 |  |
| 2-127234_2 | [+1.0 ppm, +3.0 ppm] [Zn] | 50/1 | 1.959 | 11.85 | 14.76 | 15.91 | 16.25 |
| 2-127234_1 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/3 |  |  |  |  |  |
| 2-127234_2 | [+0.5 ppm, +3.5 ppm] [Zn] | 100/3 |  |  |  |  |  |

Manufacturer: Assurance, Al lot: 27-171ALT exp: 2026-07-30

Manufacturer: Assurance, Fe lot: 28-75FEY exp: 2026-07-30

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Manufacturer: Assurance, Zn lot: 28-58ZNY exp: 2026-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]