Submission ID: 100048300

Project #: LP413RD0012

Analysis: Agilent OES and Metrohm titrator

Cr6+

| sample | weight (g) | volume (mL) | %Cr6+ | Avg(%Cr6+) | FAS=0.0924 N |
| --- | --- | --- | --- | --- | --- |
| 2-127259_1 | 1.0018 | 6.05032 | 0.967 |  |  |
| 2-127259_2 | 1.0019 | 6.40050 | 1.023 | 0.99 |  |

Cr2O3

| sample | weight (g) | volume (mL) | %Cr2O3 | Avg(%Cr2O3) | FAS=0.0924 N |
| --- | --- | --- | --- | --- | --- |
| 2-127259_1 | 0.1076 | 10.59950 | 23.077 |  |  |
| 2-127259_2 | 0.1068 | 10.52459 | 23.086 | 23.08 |  |

prep={Microwave: 10 mL H2O, 10 mL H2SO4, filter:False, for:Mg,Na, Zr}}

| sample | weight (g) | volume (mL) | Time (min) | Power (W) | T1 (°C) | T2 (°C) | P (bar) | stir |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | 0.3071 | 50 | 30 | 1500 | 250 | 65 | 110 | 90% |
| 2-127259_2 | 0.3065 | 50 |  |  |  |  |  | PTFE |

K2O

| sample | analysis prep | Dilution | conc. [mg/L] | %K | %K2O | AvgK2O |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | [0.5 ppm, 1.0 ppm] [K] | 10/6 | 0.790 | 0.02 | 0.03 |  |
| 2-127259_2 | [0.5 ppm, 1.0 ppm] [K] | 10/6 | 0.798 | 0.02 | 0.03 | 0.03 |

MgO

| sample | analysis prep | Dilution | conc. [mg/L] | %Mg | %MgO | Avg(MgO) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | [+1.0 ppm, +3.0 ppm] [Mg] | 10/1.5 | 2.378 | 0.26 | 0.43 |  |
| 2-127259_2 | [+1.0 ppm, +3.0 ppm] [Mg] | 10/1.5 | 2.329 | 0.25 | 0.42 | 0.43 |

Na2O

| sample | analysis prep | Dilution | conc. [mg/L] | %Na | %Na2O | AvgNa2O |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | [0.5 ppm, 1.0 ppm] [Na] | 25/0.7 | 0.961 | 0.56 | 0.75 |  |
| 2-127259_2 | [0.5 ppm, 1.0 ppm] [Na] | 25/0.7 | 0.951 | 0.55 | 0.75 | 0.75 |

SnO2

| sample | analysis prep | Dilution | conc. [mg/L] | %Sn | %SnO2 | Avg(SnO2) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | [+1.0 ppm, +3.0 ppm] [Sn] | 10/1.2 | 1.533 | 0.21 | 0.26 |  |
| 2-127259_2 | [+1.0 ppm, +3.0 ppm] [Sn] | 10/1.2 | 1.526 | 0.21 | 0.26 | 0.26 |

ZrO2

| sample | analysis prep | Dilution | conc. [mg/L] | %Zr | %ZrO2 | Avg(ZrO2) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127259_1 | [+1.0 ppm, +3.0 ppm] [Zr] | 25/1.5 | 2.319 | 0.63 | 0.85 |  |
| 2-127259_2 | [+1.0 ppm, +3.0 ppm] [Zr] | 25/1.5 | 2.519 | 0.68 | 0.93 | 0.89 |

Manufacturer: Assurance, K lot: 28-6KY exp: 2026-08-30

Manufacturer: Assurance, Mg lot: 28-136MGY exp: 2027-01-30

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Sn lot: 28-62SNY exp: 2026-10-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Manufacturer: Assurance, Zr lot: 28-64ZRY exp: 2026-10-30

Reference page for formulas

%Cr6+=1.733mL FAS[N FAS][weight]

%Cr2O3=1.462*[%Cr6+]

%M+=conc.volumedilutionweight*104

%MO=MWMOMWM+*%M+