Submission ID: 100048343

Project #: LC4990012

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-127372 | 27.0061 | 29.0452 | 28.9415 | 5.09 | 0.9491 |
| 2-127373 | 27.9807 | 30.0071 | 29.8945 | 5.56 | 0.9444 |
| 2-127374 | 27.1506 | 29.1514 | 29.0361 | 5.76 | 0.9424 |

prep={method:Work Instruction, filter:True, for:Ag}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127372_1 | 0.5024 | 200 |
| 2-127372_2 | 0.5049 | 200 |
| 2-127373_1 | 0.5055 | 200 |
| 2-127373_2 | 0.5065 | 200 |
| 2-127374_1 | 0.5083 | 200 |
| 2-127374_2 | 0.5090 | 200 |

prep={Katanax: Ramping, filter:True, for:Al,Si}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127372_1 | 0.2071 | 250 |
| 2-127372_2 | 0.2027 | 250 |
| 2-127373_1 | 0.2090 | 250 |
| 2-127373_2 | 0.2047 | 250 |
| 2-127374_1 | 0.2078 | 250 |
| 2-127374_2 | 0.2022 | 250 |

prep={method:Work Instruction, filter:False, for:Ru}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127372_1 | 0.3047 | 250 |
| 2-127372_2 | 0.3076 | 250 |
| 2-127373_1 | 0.3077 | 250 |
| 2-127373_2 | 0.3030 | 250 |
| 2-127374_1 | 0.3089 | 250 |
| 2-127374_2 | 0.3062 | 250 |

Ag2O

| sample | analysis prep | Dilution | conc. [mg/L] | %Ag | %Ag2O | [dried] | Avg(%Ag2O) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127372_1 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 1.654 | 0.16 | 0.35 | 0.37 |  |
| 2-127372_2 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 1.652 | 0.16 | 0.35 | 0.37 | 0.37 |
| 2-127373_1 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 2.189 | 0.22 | 0.47 | 0.50 |  |
| 2-127373_2 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 2.052 | 0.20 | 0.44 | 0.47 | 0.48 |
| 2-127374_1 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 1.429 | 0.14 | 0.30 | 0.32 |  |
| 2-127374_2 | [+1.0 ppm, +3.0 ppm] [Ag] | 25/10 | 1.436 | 0.14 | 0.30 | 0.32 | 0.32 |

Al2O3

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | %Al2O3 | [dried] | Avg(%Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127372_1 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.7 | 1.835 | 31.64 | 59.78 | 62.99 |  |
| 2-127372_2 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.7 | 1.798 | 31.68 | 59.84 | 63.05 | 63.02 |
| 2-127373_1 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.82 | 2.086 | 30.43 | 57.48 | 60.86 |  |
| 2-127373_2 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.82 | 2.037 | 30.34 | 57.31 | 60.68 | 60.77 |
| 2-127374_1 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.82 | 2.087 | 30.62 | 57.84 | 61.38 |  |
| 2-127374_2 | [+1.0 ppm, +3.0 ppm] [Al] | 100/0.82 | 2.053 | 30.96 | 58.47 | 62.04 | 61.71 |

Ru

| sample | analysis prep | Dilution | conc. [mg/L] | %Ru | [dried] | Avg(%Ru) |
| --- | --- | --- | --- | --- | --- | --- |
| 2-127372_1 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.241 | 0.20 | 0.22 |  |
| 2-127372_2 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.251 | 0.20 | 0.21 | 0.21 |
| 2-127373_1 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.284 | 0.21 | 0.22 |  |
| 2-127373_2 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.387 | 0.21 | 0.22 | 0.22 |
| 2-127374_1 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.331 | 0.21 | 0.23 |  |
| 2-127374_2 | [+1.0 ppm, +3.0 ppm] [Ru] | 10/9 | 2.474 | 0.22 | 0.25 | 0.24 |

SiO2

| sample | analysis prep | Dilution | conc. [mg/L] | %Si | %SiO2 | [dried] | Avg(SiO2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127372_1 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.330 | 1.00 | 2.15 | 2.26 |  |
| 2-127372_2 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.295 | 1.02 | 2.17 | 2.28 | 2.27 |
| 2-127373_1 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.402 | 1.02 | 2.18 | 2.31 |  |
| 2-127373_2 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.306 | 1.01 | 2.16 | 2.29 | 2.30 |
| 2-127374_1 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.390 | 1.02 | 2.18 | 2.31 |  |
| 2-127374_2 | [1.25 ppm, 2.5 ppm, 5.0 ppm] [Si] | 25/10 | 3.319 | 1.03 | 2.19 | 2.32 | 2.31 |

Manufacturer: Assurance, Ag lot: 28-66AGY exp: 2026-03-30

Manufacturer: Assurance, Al lot: 27-171ALT exp: 2026-07-30

Manufacturer: Assurance, Ru lot: 28-56RUY exp: 2026-05-30

Manufacturer: Assurance, Si lot: 28-87SIX exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]