Submission ID: 100048435

Project #: LC454RD0034

Analysis: Agilent OES

LOI

| sample | crucible | crucible+sample | after 900°C | LOI (%) | correction ƒ |
| --- | --- | --- | --- | --- | --- |
| 2-127592 | 27.9784 | 29.9792 | 29.8333 | 7.29 | 0.9271 |

prep={Hotplate:25 mL HF-off, then 60 mL HCl, filter:False, for:Al}

| sample | weight (g) | volume (mL) |
| --- | --- | --- |
| 2-127592_1 | 0.1090 | 250 |
| 2-127592_2 | 0.1068 | 250 |

prep={Microwave:9 mL HCl, 3 mL HNO3, 3 mL H2SO4, filter:True, for:Fe, Na, Zn}}

| sample | weight (g) | volume (mL) | Time (min) | Power (W) | T1 (°C) | T2 (°C) | P (bar) | stir |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127592_1 | 0.1056 | 250 | 60 | 1500 | 260 | 65 | 110 | 90% |
| 2-127592_2 | 0.1054 | 250 |  |  |  |  |  | PTFE |

Al

| sample | analysis prep | Dilution | conc. [mg/L] | %Al | %Al2O3 | [dried] | Avg(%Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127592_1 | [+1.0 ppm, +3.0 ppm] [Al] | 50/6 | 1.932 | 3.69 | 6.97 | 7.51 |  |
| 2-127592_2 | [+1.0 ppm, +3.0 ppm] [Al] | 50/6 | 1.950 | 3.80 | 7.18 | 7.74 | 7.64 |

Fe

| sample | analysis prep | Dilution | conc. [mg/L] | %Fe | %Fe2O3 | [dried] | Avg(%Fe2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127592_1 | [+1.0 ppm, +3.0 ppm] [Fe] | 50/1 | 1.894 | 22.42 | 28.83 | 31.10 | 31.10 |
| 2-127592_2 | [+1.0 ppm, +3.0 ppm] [Fe] | 50/1 | 1.692 | 20.07 | 25.81 | 27.84 |  |

Na

| sample | analysis prep | Dilution | conc. [mg/L] | %Na | %Na2O | [dried] | Avg(%Na2O) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127592_1 | [0.5 ppm, 1.0 ppm] [Na] | 250/3 | 0.830 | 16.37 | 22.07 | 23.81 |  |
| 2-127592_2 | [0.5 ppm, 1.0 ppm] [Na] | 250/3 | 0.822 | 16.25 | 21.90 | 23.62 | 23.72 |

Zn

| sample | analysis prep | Dilution | conc. [mg/L] | %Zn | %ZnO | [dried] | Avg(%ZnO) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2-127592_1 | [+1.0 ppm, +3.0 ppm] [Zn] | 50/2 | 2.064 | 12.22 | 15.21 | 16.40 |  |
| 2-127592_2 | [+1.0 ppm, +3.0 ppm] [Zn] | 50/2 | 2.008 | 11.91 | 14.82 | 15.98 | 16.19 |

Manufacturer: Assurance, Al lot: 27-171ALT exp: 2026-07-30

Manufacturer: Assurance, Fe lot: 28-75FEY exp: 2026-07-30

Manufacturer: Assurance, Na lot: 27-159NAY exp: 2026-08-30

Manufacturer: Assurance, Y lot: 28-89YX exp: 2026-10-30

Manufacturer: Assurance, Zn lot: 28-58ZNY exp: 2026-10-30

Reference page for formulas

A = crucible

B = crucible + sample

C = crucible + sample after drying

%LOI=B-[C-A]B-A*100%

000,0000M+=conc.volumedilutionweight=ppm M+

%M+=conc.volumedilutionweight*104

%M+ dried=%M+[1-%LOI100]